# BNP Gibb’s Energy for NP Shape

# Universal Theory

## Goal

The following theoretical development defines the basis required to calculate a phase diagram for bimetallic nanoparticles (BNPs). Nanoparticles’ thermodynamically stable phases are dependent on not only the temperature, composition and pressure, but also their size. Their size is dependent on the number of moles being used, as well as the BNP’s geometry. Therefore, we would like to calculate a 3D graph with the following axes:

- x axis – Composition

- y axis – Total number of moles

- z axis – Temperature

In such a graph, there may be partitions as a result of both phase and geometry changes.

## Road Map

First, we will define the parameters for which we must solve as well as identify the equations which require development. Second, we will define the equations to a degree that allows computation.

The objective is to calculate the phase diagram for given points in a loop which will cover the PD’s total scope. Every point will be defined by the PD’s axes, composition, number of moles and temperature. Mathematically, this means that for each calculation, the initial conditions will be treated as constant and given. Because the development is for BNPs, we know the following equations to always be correct:

|  | nAtotal=ntotal1-xBtotal | (1) |
| --- | --- | --- |
|  | nBtotal=ntotalxBtotal | (2) |

Where:

nAtotal – Total number of A moles in the system

Because we immediately have enough information necessary to calculate nA\Btotal we can treat them as substitutions of the other known conditions, and not variables.

We know that there are two thermodynamically stable phases at most in any given position. We also know that the total number of moles must be divided between them. Therefore, we can define eq. (3):

|  | nAtotal=nAα+nAβ | (3) |
| --- | --- | --- |

Where:

α, β – The BNP’s phases

A, B – The BNP’s types of atoms

nAα – Number of A atom moles in phase α

Eq. (3) adds 2 equations, one for each type of atom. It also introduces 4 unknown variables, depicted as all combinations of nA\Bα\β, representing the number of each type of atom in each phase.

We also define 3 additional variables which define the BNP’s geometry. The first two, rα and rβ define the size of each phase separately. A third parameter is required in order to define the interface area’s size, rα-β. How these parameters are calculated has to do with the nanoparticle shape we solve for. An in-depth example for Janus particles is given later on. We can however define an equation which describes the equality between the phases’ volumes per amount of moles and their volume by geometry, as shown in eq. (4):

|  | vAnAα+vBnBα=Vαrα,rα-β | (4) |
| --- | --- | --- |

Where –

vA – Molar volume of atom A

Vαrα,rα-β – Total volume of phase α as defined by geometric parameters

This adds an additional 2 equations, one for each phase.

Finally, we calculate for the minimum total free energy. The total free energy can be calculated as shown in eq. (5).

|  | Gtotal=Gα+Gβ | (5) |
| --- | --- | --- |

Where –

Gα\β – Total Gibb’s free energy (not per mole), function of geometry and composition

The total energy may be minimized by changing one of 3 parameters, the number of A moles in each phase, the number of B moles in each phase, and the interface’s size. Therefore, we must find the minimum energy per parameter, as shown in eq. (6), (7).

|  | dGtotaldnAα=0; dGtotaldnBα=0 | (6) |
| --- | --- | --- |
|  | dGtotaldrα-β=0 | (7) |

Eq. (6) and (7) introduce in total 3 additional equations. Thus, we have 7 parameters and 7 equations, i.e. we are able to compute once the equations themselves are defined.

## Equation Development

### Generic Nanoparticle

The bulk Gibb’s free energy for a general composition is shown in eq. (8):

|  | gγ=∑giγxiγ+RT∑xiγlnxiγ+gExγ | (8) |
| --- | --- | --- |

Where:

γ –Phase

g – Gibb’s free energy per mole

i - Type of atom in the composition

x – Molar concentration

R  - Gas constant

T  - Temperature

gEx - Excess energy from interatomic interactions per mole

For nanoparticles we must add an additional variable to account for the surface energy. This energy is typically negligible when dealing with large quantities of materials, however in nanoparticles it is not at all negligible. The result is shown in eq. (9):

|  | gnanoγ=gγ+gsurfr,x=∑giγxiγ+RT∑xiγlnxiγ+gExγ+gsurfγ | (9) |
| --- | --- | --- |

Where –

gsurfr,x – Surface energy per mole (a function of both size, r, and composition, x)

In order to calculate the chemical potential, we must calculate the total energy (i.e. not per mole) as shown in eq. (10):

|  | Gnanoγ=gγnA+nB=Σgiγniγ+RTΣniγlnniγΣniγ+GExγ+Gsurfγ | (10) |
| --- | --- | --- |

### BNP Gibb’s free energy

For a BNP, there are only two atoms – A, B. Also, at most two phases can be stable simultaneously - α, β. Therefore, the system’s free energy can be described as shown in eq.  (11):

|  | Gtotal=Gα+Gβ | (11) |
| --- | --- | --- |

Where the total free energy of a specific phase is now described as shown in eq. (12):

|  | Gα=gAαnAα+gBαnAα+RTnAαlnnAαnAα+nBα+nBαlnnBαnAα+nBα+GExα+Gsurfα | (12) |
| --- | --- | --- |

The molar Gibb’s free energy of a pure material in a given phase is known and found readily available in literature, namely the SGTE database. Likewise, the excess molar Gibb’s free energy can be calculated as described by Redlick-Kister, with interaction parameters existing in the literature.

### Surface Energy

For a generic state of n phases, the surface energy of phase γ, is defined as shown in eq. (13):

|  | Gsurfγ=σγAγ+δ≠γσδ-γAδ-γ | (13) |
| --- | --- | --- |

Where:

σγxiγ – Surface energy of γ with vacuum.

Aγxiγ, rγ, rγ-δ - Surface area of γ in contact with vacuum.

σδ-γxiγ,xiδ – Surface energy of γ in contact with δ

Aδ-γxiγ, rγ, rγ-δ – Surface area of γ in contact with δ

rγniγ,vi  - ‘Radius’, a place holder used to define geometry of γ

rγ-δ  - ‘Radius’, a place holder used to define geometry of the contact area

ni – amount of moles on atom i

For a BNP, eq. (13) can be simplified to eq. (14):

|  | Gsurfα=σαAα+0.5σα-βAα-β | (14) |
| --- | --- | --- |

Calculating the different surface areas, A, is dependent on the BNP’s geometry. An example will be shown for Janus particles later.

### Composition’s Surface Energy

Calculating the total energy accurately, and through it the phase diagram, requires that we enter correct values for the surface energy. This cannot be done by simply taking values from the literature, because those values don’t properly account for the changes in surface energy as a result of composition changes.

In order to calculate the surface energy as a function of the composition, and then by extension by number of atoms in each phase, we use a simplified Butler equation. The non-simplified version is shown in equations (15), (16):

|  | σcompositionα=σApure+RTAAmolarlnxAsurfxAbulk+1AAmolarGAE,surf-GAE,bulk | (15) |
| --- | --- | --- |
|  | σcompositionα=σBpure+RTAAmolarlnxAsurfxAbulk+1ABmolarGBE,surf-GBE,bulk | (16) |

Where:

Ai  - Partial molar surface area of a monolayer of i

xsurf – Composition at surface

For which Ai can be described as follows:

|  | Aimolar=1.091NA13vi23 | (17) |
| --- | --- | --- |

Where:

NA – Avogadro’s number

vi – Molar volume of atom i

We calculate for a simplified version, where the surface composition is similar to the bulk composition. As such, we make the claims shown in equations (18), (19):

|  | xsurf=xbulk+δ | (18) |
| --- | --- | --- |
|  | GiE,surf=GiE,bulk | (19) |

Which reduces equations (15), (16) to:

|  | σcompα=σApure+RTAAln1+δxAα | (20) |
| --- | --- | --- |
|  | σcompα=σBpure+RTABln1-δ1-xAα | (21) |

By developing a Taylor series around the previously stated assumption the difference between surface and bulk composition is small, i.e. δ is very small, equations (20), (21) become:

|  | σcompα=σApure+RTAA∙δxAα | (22) |
| --- | --- | --- |
|  | σcompα=σBpure-RTAB∙δ1-xAα | (23) |

Since the LHS of both equations (22) and (23) are identical, we can equate them, as shown in equation (24):

|  | σApure+RTAAδxAα=σBpure-RTABδ1-xAα | (24) |
| --- | --- | --- |

From which the term δ can be extracted, and shown to be:

|  | δ=σBpure-σApureRT∙AAABxAα1-xAαAAxAα+AB1-xAα | (25) |
| --- | --- | --- |

This value can be substituted into equation (22), so as to calculate the surface energy value as a function of composition. The result is shown in equation (26):

|  | σcompα=σApure+σBpure-σApureAB1-xAαAAxAα+AB1-xAα | (26) |
| --- | --- | --- |

Equation (26) can be rewritten to be more readable, as shown in equation (27):

|  | σcompα=AAxAαAAxAα+ABxBασApure+ABxBαAAxAα+ABxBασBpure | (27) |
| --- | --- | --- |

This equation can be simplified further by inserting the definition of A as explained in equation (17), which leads to the reduction of the constant and Avogadro’s number, leading to (28).

|  | σcompα=vAα23xAαvAα23xAα+vBα23xBασAαpure+vBα23xBαvAα23xAα+vBα23xBασBαpure | (28) |
| --- | --- | --- |

This solution represents the value for a certain phase with vacuum. A more generalized solution can be found for the interface between phases α, β through similar algebra. The end result is presented in equation (29).

|  | σαβ=i,j=A,Bviα23xiαvAα23xAα+vBα23xBα∙vjβ23xjβvAβ23xAβ+vBβ23xBβσiαjβ | (29) |
| --- | --- | --- |

This generalized solution shows how to calculate the surface energy of any composition interacting with a different composition based on the surface energy of pure materials interacting. This enables the use of readily available results from literature regarding the surface energy of different pure materials with the relevant materials for which we would like to calculate.

# Specific Situations

## Janus Particle

### Standard Geometry’s Definition

For a Janus particle which has the above geometry, we can calculate the volume values as follows:

|  | Vblue=vAbluenAblue+vBbluenBblue=16πhblue3a2+hblue2 | (30) |
| --- | --- | --- |

Where:

h - rα-β for this case

r - rα for this case

vA\B - Pure material’s molar volume

From these parameters we may calculate the surface areas:

|  | Ablue=πa2+hblue2 | (31) |
| --- | --- | --- |
|  | Ared-blue=πa2 | (32) |

### Development for BNP PD Calculation

From eq. (30) we can see that the value of h is defined by three parameters, nA, nB, and a, i.e. h changes to the correct size which contains all atoms in the phase for the given interface size.

We define a as an independent variable. This is because the interface could potentially be of varying size for the same amount of atoms, depending on the minimum energy.

In order to calculate the derivatives of h, we use the known equation to differentiate implicit functions Fx,yx=0 shown in equation (33):

|  | ∂y∂x=-∂F∂x∂F∂y | (33) |
| --- | --- | --- |

First, we rewrite equations (30) so that every term appears on the left hand side.

|  | Fblue=vAbluenAblue+vBbluenBblue-16πhblue3a2+hblue2 | (34) |
| --- | --- | --- |

From here, we derive according to eq. (33). The results are shown in eq. (35), (36).

|  | ∂hblue∂nAblue=2vAπa2+hblue2 | (35) |
| --- | --- | --- |
|  | ∂hblue∂a=-2ahbluea2+hblue2 | (36) |

We can describe rα to be either hred or hblue depending on the geometry we would like to solve for, and have rα-β be a, leaving us with completely solvable equations.

## Equation Simplification

While the general solution can be applied to all systems, simplifying the equations is often possible and advantageous with regards to calculation resources.  For some geometries, such as core-shell ones, the simplification is straightforward. All geometric parameters are clearly defined by the amounts of moles in the inner and outer phases, i.e. there is no free interaction size parameter.

In the case of Janus particles for example, we can simplify the rinterface parameter as follows. First, let’s look at the equation for the total Gibbs free energy of a nano particle, as shown in equation (37).

|  | Gtotal=Gbulkα+Gbulkβ+Gsurface | (37) |
| --- | --- | --- |

In equation (37) only the third parameter, Gsurface, is a function of rinterface, or any geometric variable for that matter. Therefore, when we differentiate (as part of equation (7)) as shown in equation (38), we get the result shown.

|  | dGtotaldrinterface=dGbulkαdrinterface+dGbulkβdrinterface+dGsurfacedrinterface=dGsurfacedrinterface=0 | (38) |
| --- | --- | --- |

We can describe the total Gsurface as shown in equation (39).

|  | Gsurface=Gαvacuum+Gβvacuum+Gαβ=Aασα+Aβσβ+Aαβσαβ | (39) |
| --- | --- | --- |

Where –

Aγ – Area of a phase with vacuum

σγ – Surface energy of a phase with vacuum

Aαβ – Interface area between phases

σαβ – Surface energy at interface between phases

Inserting equation (39) into equation (38) leads to equation (40).

|  | dGsurfacetotaldri=dAαdriσα+dAβdriσβ+dAαβdriσαβ=0 | (40) |
| --- | --- | --- |

This result stems from the fact that the surface energies aren’t functions of any specific geometry, as shown in the development in equation (29). By implementing the definition of Aα as shown in equation (31) as well as the necessary differentiation shown in equation (36), we can calculate the differentiation shown in the following equation.

|  | dAαdri=∂Aα∂ri+∂Aα∂rα∙∂rα∂ri=2πriri2-rα2ri2+rα2 | (41) |
| --- | --- | --- |

For the interface, the solution is as shown in equation (42).

|  | dAαβdri=2πri | (42) |
| --- | --- | --- |

Inserting equations (41), (42) into equation (40) can be solved algebraically, the result is shown in (43).

|  | σα+σβ+σαβari22+rα2+rβ2σαβ-σα-σβrα2-rβ2σαβbri2+rα2rβ2σαβ-σα-σβc=0 | (43) |
| --- | --- | --- |

This equation can be solved as a quadratic solution for the variable ri2, thus enabling us to substitute ri for its solution as function of the other parameters. This not only allows us to shorten the time required for the calculation, but also shines light onto the problem’s physics. Through this solution, we understand that there is a formula for the optimal geometrical solution.